## Slide 1: Overview of new devices in the era of Beyond CMOS
2024/05/14
MegaChips Corp
yoshitomi.sadayuki@megachips.co.jp

## Slide 2
Keywords of device developments for 2030
Spectrum
&
Interference
Management
BY Cognitive
Signal
Conditioning
Training
Smart DPD
Antenna
Integration
More than Moore
Speed/Linearity/Noise
Smart-DPD
Algorithm
Dense Integration/
Speed/Power
More Moore
Speed/Power
Beyond CMOS

## Slide 3
Portfolio of Extended CMOS developments.
+ Performance for digital
Further scaling of MOSFETs
to improve the performance of LSIs.
-> new materials and structures are
essential.
+ Increase the add value
-> Integrate various functions
(RF, power, passive elements,
sensors, actuators)
other than digital logic into LSIs.
+ Improve the performance
-> using devices that operate
on a different principle to
MOS transistors.

## Slide 4: Contents
2. New materials and structures for further scaling
of MOS transistors.
1. Throw back to the era of MOS transistors’ scaling.
3. Fighting with Layout Parasitic Elements to conquer
More than Moore.

## Slide 5: Throw back to the era of MOSFET scaling

## Slide 6
Source
Drain
Gate
LG
Electrical Field = Constant
TOX
WD
Depletion
Layer Width
Impurity Concentration
in the Channel (substrate)
Na
Source
Drain
Gate
αNa
WD/α
LG/α
TOX/α
VDD/α
Width W/α
Before
After
Integrated Density → α2
Delay → 1/α
Power consumption/Device → 1/α2
R.H Dennard et al., IEEE JSSC 9, 256 (1974)
Revisit to R.H Dennard’s scaling rule (~ 50 Years)

## Slide 7
Source
Drain
Gate
Current
Channel (Inversion Layer)
NMOS-Electrons
PMOS-Holes
Why we cannot realize what we want ?
What is a problem and how to solve this ?
Gap between theory and reality..
IOFF
ION
IS
Subthreshold region
VGS
Log10(ID)
We want this !
But..

## Slide 8
IOFF↑ Leak increases.
Source
Drain
Gate
IJ
ION
IG
IS
Scaling
IOFF
ION
IS
Subthreshold region
↑（IG）Gate Leak Current
↑（IJ）Junction Leak S/D and Backgate
↑（IS）Subthreshold Leak ← Short-channel Effect
Challenges in MOSFETs Scaling (1/2)
VGS
Log10(ID)

## Slide 9
Ion degrades from the expectation
Source
Drain
Gate
ION
IG
DC: Leveling off due to impurity scattering.
AC:Parasitic R/C in MOSFET and BEOL
Mobility
Concentration
Velocity
Unwanted Increase of variation
-σ（VTH） ↑ Due to larger
-σ（Leff) ↑ Due to Lithography Process
Ninv : from Boltzmann statistic
to discretized numbers
Challenges in MOSFETs Scaling (2/2)
σNinv

## Slide 10
Source
Drain
Gate
IJ
ION
IG
IS
Footprints of innovation of planar CMOS
Source
Drain
Gate
IJ
ION
IG
IS
Source
Drain
Gate
IJ
ION
IG
Source
Drain
Gate
IJ
ION
IG
IS
High-K
Dielectric Film
Low-K
Dielectric Film
Cupper Metal
Mobility Enhancement
Strained Silicon
Gate Leak Reduction
Silicon On Insulator
Reduction of channel to Body Capacitance.
Low parasitic BEOL (Back End Of Line)
Reduction of propagation delay of BEOL.
Lots of innovations are well done for planar CMOS.
Go to a next step for a new era !

## Slide 11
Metal Gate
/High-K dielectric gate insulator
Effective thickness of Gate
Insulator ~ 0.95nm
C.H Jan et al., (Intel) IEDM2008, p.637
P.Packan et al., (Intel) IEDM2009, p.659
Intel’s 32nm Generation MOSFET

## Slide 12: New materials and structures for further scaling of MOS transistors.

## Slide 13: Strategy of enhancement for higher on current.
Mobility
Channel
Doping
Velocity
・Explore for high mobility
-Strained Silicon.
-SiGe, Ge
- Ⅲ-Ⅴ materials.
-Carbon Nano-Tube, Graphene.

## Slide 14: Mobility Benchmark
Better performance is expected:
Ge-PMOS, Ⅲ-Ⅴ NMOS
Narrow Bandgap → Leak Current（IJ）↑
 | Si | Ge | GaAs | InAs | InSb
Electron (cm2/Vs) | 1600 | 3900 | 9200 | 40000 | 77000
Hole (cm2/Vs) | 430 | 1900 | 400 | 500 | 850
Band-gap (eV) | 1.12 | 0.66 | 1.424 | 0.36 | 0.17
Pros
Cons

## Slide 15: Ge pMOSFET
・Leakey nature of Gate insulator (GeO2)
・Large Leak current (Ij)
・More explore is required for NMOS.
J. Mitard et. al, ”Record ION/IOFF performance for 65nm Ge pMOSFET
and novel Si passivation scheme for improved EOT scalability”,
DOI: 10.1109/IEDM.2008.4796837
Issues

## Slide 16: Ⅲ-Ⅴ MOSFET
・High density of interface states
→ gm degradation.
・Device fabrication on Si substrate.
https://studylib.net/doc/18330212/advanced-cmos-scaling
Issues

## Slide 17: The era of Nano-Wire
・Nano-Wire=1-dimensional channel.
Source
Ballistic
Transport
Channel
Drain
Current
・Carrier can move toward 1-D direction.
→Less chance to meet phonon scattering.
→Potential for Ballistic-Transport（no Scattering）
Nano-Wire

## Slide 18: Carbon-Nano-Tube
1 dimensional transport.
Mobility：36000cm2/Vs
Mechanically stable, high thermal conductivity.
Difficult to control Chirality.
Diameter~1.2nm
Length~Several um
Six-membered-Ring
Roll
CNT
Graphene
few nm
Pros
Cons

## Slide 19: CNT MOSFET
Solvent of CNT is spread on the film
of oxidized materials for device fabrication.
Davood Shahrjerdi et. Al,”High device yield carbon nanotube NFETs for high-performance logic applications” IEDM 2011.

## Slide 20: Chirality of CNT
P.G Collins et.al.(IBM) Science 292, 706 (2001)
What happens when applying large bias.
Metallic part → Breakdown occur.
Semiconductor part→ Keep the same nature.
Vg［Ｖ］
Conductivity
[Siemens]
0
Before
（Metallic Nature → Normally-On）
After
（Semiconductor Nature → Normally Off）

## Slide 21: FinFET, Nano-Wire and Gate All Around
FinFET
Fin-Channel
Gate
Fin-Channel
Gate
Nanowire-Tr
SiO2
Si
SiO2
Si
Fin Width 10-20nm
Fin Height 25-50nm
Fin Width 10-15nm
Fin Height 10-15nm
Fin-Channel
Gate
SiO2
Si
Fin Width (dNW)
5,10,20,30,40 nm
Fin Height (HNW) 22 nm
Anshul Gupta et.al,"Time Evolution of DIBL in
Gate-All-Around Nanowire MOSFETs During
Hot-Carrier Stress", IEEE Transactions on ED
(2021),Vo.68,Issue 6
Gate-All-Around Tr
Nanowire devices successfully take over More than Moore
era,

## Slide 22: Fighting with Layout Parasitic Elements - To beat the era of “More than Moore” -

## Slide 23: Figure Of Merit comparison toward 7nm
Chart: Analog FoM
| 16 | 22 | 32 | 45
Analog FOM (NMOS+PMOS)(HP+LP) | 2.239 | 2.0558 | 1.7492 | 1.4006
Analog FOM (NMOS+PMOS)(HP+LP) | 3.4591 | 2.9678 | 2.4862 | 1.9867 | 1.6135
Chart: Digital Dynamic Power
| 16 | 22 | 32 | 45
Digital Dynamic Power (NMOS+PMOS)(HP+LP) | 37.0117 | 53.7022 | 77.8411 | 110.8332
Digital Dynamic Power (NMOS+PMOS)(HP+LP) | 13.042 | 12.4147 | 15.3626 | 18.4112 | 21.5026
Chart: Leakage Power
| 16 | 22 | 32 | 45
Digital Leakage Power (NMOS+PMOS)(HP+LP) | 711.3689 | 183.166 | 60.8369 | 24.6586
Digital Leakage Power (NMOS+PMOS)(HP+LP) | 207.5638 | 136.9066 | 146.2931 | 155.028 | 163.6919
BULK-CMOS
Fin FET
FinFET
BUK-CMOS
7nm
7nm
7nm
Reference
https://keep.lib.asu.edu/items/157985
Predictive Process Design Kits for the 7 nm and 5 nm Technology Nodes
FinFET technology outperforms BULK-CMOS in all FoMs.
But The FOM tends to level off around 7nm node.

## Slide 24: Price of Logic Density – Parasitic increase below 7nm -
Chart: 
| 40 | 28 | 16 | 7 | 5
MX Resistance | 1 | 2 | 7 | 21 | 63
MX Capacitance | 1 | 0.95 | 0.89 | 1.1 | 1.14
40nm
28nm
16nm
7nm
5nm
Mx Resistance (vs. 40nm)
Mx.R
Mx.C
Alvin Loke ,”ISSCC 2024 - Forum 3.1: Extending and Augmenting Analog with Digital to Overcome Technology Scaling Limitations”
X3
X3
Mx Capacitance (vs. 40nm)
Resistance
 Rinterconnects (mainly MEOL & lower BEOL)
 Rcontact & Rvia ➜︎ severe IR droop
 Rgate ➜︎ non-quasistatic effects
 Rwell ➜︎ well-ties, latchup
Capacitance
 Strong gate coupling to S/D contacts & overlying metal

## Slide 25: Strategy of fighting Layout Parasitics (1/2)
D
S
S
D
S
S
SA
STI_W
Cgd
Cgs
Cgd
Cgs
Cgs
Cgd
SB
SD
STI_L
+ Well Proximity Effects

## Slide 26: Compact Model Features
M1 1=D 2=G 3=S 4=B MOSMOD L=0.25u W=5u NF=1
AD=5p AS=5p PD=12u PS=12u NRD=0 NRS=0
SA=SA_val SB=SB_val SD=SD_val
SCA=SCA_val SCB= SCB_val SCC= SCC_val SCD= SCD_val
DELVTO=f(STI_L, STI_W,..) Mulu0= g(STI_L, STI_W,..)
.MODEL MOSMOD NMOS
LEVEL = 14
VERSION = 4.3.0
BINUNIT = 2
….
+MOBMOD = 1 RDSMOD = 0 IGCMOD = 0 IGBMOD = 0 CAPMOD = 2
+ RGATEMOD = 1 RBODYMOD = 1 TRNQSMOD = 1 ACNQSMOD = 1
+ TNOIMOD = 1 DIOMOD = 1 PERMOD = 1 GEOMOD = 0
…….
+SAREF = 5E-6 SBREF = 5E-6 KU0 = -4E-6
+KVSAT = 0.2 KVTH0 = -2E-8
….
Back annotated
after parasitic extraction
- Available in the
Schematic symbols
- Synchronized with p-cell
f() and g() are customized functions describing
VTH0 and U0 shift.

## Slide 27: LDE Effect : How it shows up ?
Small
Stress effect
Fine Gate pitch
Stress effect
Fine Gate pitch

## Slide 28: Working with the reduction of R/C parasitic elements for higher cutoff frequency (fT and fMAX).
Narrow < 1um CGB , Rg
Sweet Spot ~1um
Wide > 1um Rg
Long distance: CGD Rg
D
S
S
Cgd
Cgs
D
S
S
Cgd
Cgs
Cgs
SD
Distance
Negligible impact.
W
NQS
Effect
Long distance: CGD CJ
SD
Negligible impact.
Drain Routing Metal
Try to use as far routing layer as from the Gate electrode.
CGD

## Slide 29: Layout optimization for the Tr speed faster than Moore’s prediction.
https://kobaweb.ei.st.gunma-u.ac.jp/lecture/20210729_analog_KIOXIA_Yoshitomi.pdf

## Slide 30: Summary
More than Moore and Beyond CMOS toward 2030.
- New materials
- 1 dimensional carrier Transport may play a dominant
role. Linking to the GAA (Gate All Around) devices.
- Overcome the parasitic R/C influence owes designers’
technique.